Comments on optical system for calibration
Jan Smolik, Jaroslav Zalesak
Institute of Physics, Prague

---
Present system: one tile – one optical fibre
 → it is very complicated system
Idea: use one fibre for more tiles, ideally one row of tiles – one fibre
How to do it?
Side-emitting fibre
Classical end-emitting fibre with some “damage” effecting side-lighting

---
Side-emitting fibres
In principal the easiest solution – to buy, lace through tiles and connect to LED driver
Problem to find thin (~1mm) fibres for test moreover not know parameters of this fibres
Price ? (Higher than for standard fibres)
Non-uniformity of light in tiles (attenuation)
Need to focus enough LED light into fibre (~100 more than present)

---
Side-emitting fibre
Test: SLL600UVT from FiberTech - Germany
(long-length side-emitting fibre)

---
Classical fibres
Low costs – many suppliers
Need additional modification to produce side light – remove cladding or to bend fibre
(< minimum bending radius, curvature shape?)
More complicated installation
Need to focus enough LED light into fibre

---
Classical fibres
Test: CK40 from Mitsubishi Rayon Corporation

---
Classical fibres
“Processed” fibre – light emitting
rubbing
fibre end
Bending

---
Conclusion
Both fibres generate signal in tiles – from side-emitting is smaller – need to test a different type (getting short-length fibre)
About to test new UV/Blue LEDs to get enough light
For developing of system for new prototype of TileHCAL we need at least two tiles with SiPM detectors and readout electronics